## Slide 1
NEWERA
Presenter: Hou Zhiwei
Application Technology Report
On Fluorosilicone Materials

## Slide 2
01
Overview of Fluorosilicone Materials
02
Fluorosilicone Materials Family
03
Key Applications
04
Company Profile
CONTENT

## Slide 3
ONE
01
Company Profile

## Slide 4
New Era Chemical Shandong Co., Ltd., located in Weihai City, Shandong Province, China, is a professional manufacturer of organic fluorosilicone fine chemicals and fluorosilicone materials. The company has established a complete industrial chain spanning from “Tetrachloroethylene → Trifluoropropene → D3F → Fluorosilicone Rubber and Fluorosilicone Oil.” It is recognized as a National-Level “Specialized, Refined, Distinctive, and Innovative” Small and Medium-sized Enterprise.
01
Company introduction

## Slide 5
TWO
02
Overview of Fluorosilicone Materials

## Slide 6
The genetic code of
fluorosilicone materials
Fluorosilicone materials are fluoropolysiloxanes characterized by a siloxane (Si–O) backbone and side chains containing both trifluoropropyl and methyl groups.
They integrate the key strengths of their parent materials: the exceptional heat resistance, low‑temperature flexibility, weathering stability, and electrical insulation of silicones, together with the superior resistance to hydrocarbons, oils, and chemicals, combined with low surface energy, inherent to fluorinated compounds.

## Slide 7
Fluorosilicone Materials: Multi-dimensional Performance
High-temperature resistance
225 ℃
( 250 °C peak )
Multifunctional chemical resistance
Including fuels, lubricating oils, hydraulic fluids, solvents, and chemicals.
Outstanding durability
Excellent resistance to weather, ozone, and aging
Safe, Eco-friendly
low temperature resistance
( Brittleness Temperature
-62 ℃ )
Non-toxic, and Odorless.

## Slide 8
THREE
03
Fluorosilicone Materials Family

## Slide 9
Methyl
Fluorosilicone Oil
D3F
Fluorosilicone Oil
2025年
Fluorosilicone Rubber
High-Temperature Vulcanized
Fluorosilicone Rubber
Hydroxyl
Fluorosilicone Oil
Vinyl
Fluorosilicone Oil
Si‑H Functional Fluorosilicone Oil
Liquid
Fluorosilicone Rubber
Fluorosilicone oil and fluorosilicone rubber are synthesized via polymerization of D3F cyclic trimer.

## Slide 10
Fluorosilicone Oil
Characteristics：Hydroxyl-terminated fluorosiloxane polymer
Applications： Used as the structuring control agent for fluorosilicone rubber, and as the base gum or diluent for condensation‑cure, room temperature vulcanizing (RTV) fluorosilicone rubber.
Characteristics：Methyl-terminated fluorosiloxane polymer
Applications： Used as a defoamer, lubricant, and high‑voltage cable insulating fluid; also functions as a release agent, barrier coating agent, and gloss enhancer.
Hydroxy Fluorosilicone Oil
Methyl Fluorosilicone Oil

## Slide 11
Fluorosilicone Oil
Characteristics: Vinyl‑terminated fluorosiloxane
Applications：Base gum for addition-cure fluorosilicone rubber
Characteristics： Si‑H (silane‑hydride) terminated fluorosiloxane polymer.
Applications： Functions as a crosslinker for addition‑cure fluorosilicone rubber and as a water‑repellent agent for substrates like rubber and metal.
Vinyl Fluorosilicone Oil
Si‑H Functional Fluorosilicone Oil

## Slide 12
A liquid, addition-curable polymeric material composed of vinyl-functionalized polyfluorosiloxane as the base polymer and hydrosilyl-terminated oligomeric fluorosiloxane as the crosslinker.
Liquid Fluorosilicone Rubber
A solid compound formulated with a fluorosilicone elastomer gum base, reinforced with silica and modified by structuring control agents and other additives.
High-Temperature Vulcanized Fluorosilicone Rubber
02
01
Fluorosilicone Rubber
A hybrid material combining silicone rubber and fluoroelastomer

## Slide 13
Solid Compound | Basic Form | Liquid, Two‑Part A/B System
Compression molding, Calendering, Extrusion | Processing Method | Injection Moulding
Peroxide Curing | Curing Mechanism | Platinum-Catalyzed Addition Curing
Low | Product Complexity & Precision | Extra-high
Can be produced on a plate vulcanizer; simple mold structure, low cost. | Mold & Equipment Cost | Requires a dedicated LSR injection molding machine; high‑precision molds, high cost.
Liquid Addition-Cure
Fluorosilicone Rubber
High-Temperature Vulcanized Fluorosilicone Rubber
VS

## Slide 14
Resilience >35%, Suitable for manufacturing umbrella valves, duckbill valves, O‑rings, diaphragms, and similar components.
High-Resilience
Fluorosilicone Rubber
01
Offers excellent tensile and tear strength, making it ideal for damping elements and dynamic, fatigue‑resistant parts.
High-Tear-Strength
Fluorosilicone Rubber
02
When used with a dedicated primer, it achieves excellent adhesion to metals, nylon, and other substrates.
Metal‑ / Nylon‑Bondable
Fluorosilicone Rubber
03
Features excellent bondability to silicone rubber, enabling the production of turbocharger hoses and other composite hose assemblies.
Turbocharger‑Hose‑Grade Fluorosilicone Rubber
04
HTV Fluorosilicone Compound Segmentation

## Slide 15
Excellent flame‑retardant properties, achieving a UL94 V‑0 rating.
Flame-Retardant Series
Fluorosilicone Rubber
05
Features exceptional resistance to transformer oil with a dielectric loss < 0.5%.
Transformer-specific
Fluorosilicone Rubber
06
Excellent extrusion processability for manufacturing a wide range of hoses.
07
Possesses a high safety profile and is suitable for food‑contact applications.
Addition-type
Fluorosilicone Rubber
08
HTV Fluorosilicone Compound Segmentation
Extruded Series
Fluorosilicone Rubber

## Slide 16
Fluorosilicone Rubber: Heat Resistance
Chart: 
| 150 ℃×72h | 200 ℃×72h | 225 ℃×72h | 250 ℃×72h
空白 | 10 | 22 | 40 | 80
添加耐热剂 | 10 | 18 | 24 | 60
Without Heat-Resistant Stabilizer
With Heat-Resistant Stabilizer
Effect of Heat-Resistant Stabilizers on Fluorosilicone Rubber
Test Condition
Change in tensile strength
Fluorosilicone rubber is rated for continuous service at 200 °C. Above this temperature, thermal cleavage of the siloxane backbone occurs, degrading mechanical properties. Formulation with heat‑resistant stabilizers is necessary to improve its thermal‑oxidative stability.

## Slide 17: Fluorosilicone Rubber Curing Systems
It offers a wide curing temperature range (both high and low). Suitable for applications demanding extreme purity, such as medical, food‑contact, high‑end electronics, and high‑clarity products.
Platinum‑Catalyzed
03
Curing temperature range: 100—120 °C. Applied in processes such as hand‑lay‑up coating and extruded rubber hose manufacturing.
DCBP
02
Used for compression/injection molding at 160—170 °C. A cost‑effective solution for general industrial parts, automotive seals, and O‑rings in price‑sensitive applications.
DBPH
01
The curing systems for fluorosilicone rubber include peroxides (DBPH, DCBP) and platinum‑catalyzed addition cure. Each offers distinct properties for different application needs.

## Slide 18: Comparison of Fluorosilicone Rubber Processes
Process Type | Compression Molding | Injection Molding | Extrusion Molding | Coating / Cladding
Product Shape | Medium Complexity | High complexity | 2D Constant cross-section | Complex Substrate Surface
Dimensional Accuracy | Good | Excellent | Fair | Process‑ Dependent
Production Efficiency | Low-Medium | Very High | Very High (Continuous) | Low
Mould/Equi-pment Cost | Low-Medium | High | Medium | Medium-High
Key Applications | Seals, Gaskets | Precision Parts, Oil Seals | Sealing Strips, Hoses | Rubber-covered roll, Hoses

## Slide 19
FOUR
04
Application Fields of Fluorosilicone Materials

## Slide 20
Multiscenario Applications of Fluorosilicone Rubber
Automotive
Critical seals for engines, Transmission, and fuel systems.
Aerospace
Seals & Protective Coatings for Fuel Lines, Hydraulic Systems, Engine Bays
Petrochemical
Bionic Robots
Wearables
Watch Straps, Wristbands, Device Seals, Waterproof Components
O-rings, Valve Gaskets, Reactor Lid Seals, Storage Tank Roof Seals, Pipeline Seals
Cosmetics Packaging
Bottle Cap Liners, Pump Seals, Tube Connector Seals
New Energy
—Critical Sealing & Flexible Components in Demanding Environments

## Slide 21: Fluorosilicone Rubber’s Core Advantage in Automotive Applications
01
It can operate stably for extended periods at temperatures above 200 °C, ensuring that pipelines do not age or deform under extreme operating conditions.
Excellent High-Temperature Resistance
02
It exhibits strong corrosion resistance to fuels, engine oils, lubricants, and exhaust environments.
Excellent Oil and Chemical Resistance
03
Through formulation design, fluorosilicone rubber can achieve strong adhesion to substrates such as silicone rubber, metals, and nylon.
Excellent Adhesion to Silicone Rubber and Metals

## Slide 22: Core seals for Engine, Transmission, and Fuel System
Fuel line O-rings, injector seals, fuel tank float seals
Fuel System Applications
Turbocharger hoses, bellows, valve stem seals
Engine System Applications
Transmission seals, gaskets, and oil seals
Transmission Applications

## Slide 23: Performance of Fluorosilicone Rubber in Automotive Oil-Contact Environments
Oil Type | Test Condition | Rate of volume change
Diesel | 80 ℃×336 h | 7~10%
Biodiesel(B20) | 80 ℃×336 h | 7~10%
RME (DIN14214) | 125 ℃×72 h | 8~10%
Engine oil（5W30） | 150 ℃×168 h | 2~3%
Brake Fluid（DOT3） | 120 ℃×72 h | 2~4%
Lubricating oil（206304） | 150 ℃×94 h | 2~3%
ASTM C | 23 ℃×72 h | 19~27%
FAM B | 23 ℃×72 h | 24~30%
IRM 903 | 150 ℃×72 h | 2~3%

## Slide 24
Automotive Applications
Exhaust Gas Valve
Bellows
Turbocharger Hose
Seals

## Slide 25
Applications in Chemical and Power Industries
Acid and Alkali Resistance
Suitable for acid/alkali-resistant piping, unaffected by corrosive chemicals.
Solvent Resistance
Used in valve seals, coating seals, and tank roof seals, offering excellent resistance to solvents.
Weather Resistance
Ideal for outdoor cable sheathing, providing long-term oxidation resistance to ensure reliable power transmission.
Transformer Oil Resistance
Applied in transformer seals, with a dielectric loss of <0.5% in transformer oil.

## Slide 26
Medium
Test Condition
1
2
3
4
5
6
7
8
10 wt% HCl solution
Concentrated HCl
10 wt% HNO₃ solution
10 wt% NaOH solution
50 wt% NaOH solution
Ethanol
Xylene
Carbon tetrachloride
23 ℃×168 h
23 ℃×168 h
23 ℃×168 h
23 ℃×168 h
23 ℃×168 h
23 ℃×168 h
23 ℃×168 h
+2
+8
+1
+1
+2
+5
+20
详情
详情
23 ℃×168 h
+20
Resistance to Solvents, Acids, and Alkalis of Fluorosilicone Rubber
Volume Swell /%

## Slide 27
Sealing for Extreme Operating Conditions in Aerospace
Resistant to extreme temperatures
Resistance to Fuels and Chemicals
Applications include fuel tank seals, O-rings, refueling valve gaskets, and fuel lines.
Liquid Fluorosilicone Rubber (LSR) is also used as a surface coating, lubricant, sealant mastic, and adhesive.
Operating range approximately –60 °C to +230 °C, with short‑term resistance above 250 °C.
Exhibits excellent resistance to jet fuels (JP‑4, JP‑8), solvents and other chemicals.
Resistance to Ozone and Nuclear Radiation
Resistant to ozone, UV & space radiation, suitable for external spacecraft components.

## Slide 28
Oil Type
Test Condition
Volume Change Rate/%
1
2
3
4
RP-3（Jet A-1）
RP-3（Jet A-1）
AMS 2629
AMS 3021
65 ℃×24 h
175 ℃×72 h
23 ℃ /22 h
150 ℃ /70 h
+5
+12
+21
+12
详情
详情
详情
Test Condition
Test result
5
Ozone resistance (aging)
200×10-8，40 ℃×72 h， 20%Tensile
No cracking
Performance
Performance of Fluorosilicone Rubber in Aerospace Applications

## Slide 29
Smart Wearables
Watch Bands: All‑Day Comfort
Hypoallergenic and resistant to sweat, oils, alcohol, and cosmetics; easy to clean and disinfect.
Housing/Seals: Superior Water & Dust Resistance
Effectively protects internal electronics from moisture and dust, significantly extending product lifespan.
Medium | Test Condition | Volume Swell /%
Oleic acid | 23 ℃×24 h | ＜1%
Artificial sebum | 23 ℃×24 h | ＜1%
Artificial Sweat | 23 ℃×24 h | ＜1%
Fluorosilicone materials are key to enhancing the durability, safety, and premium feel of high‑end smartwatches and fitness trackers.

## Slide 30: Applications in Cosmetics
Lipstick Molding Tube
（Addition-type liquid fluorosilicone rubber）
Essential oil | Test Condition | Volume Swell /%
Gardenia Essential Oil | 23 ℃×24 h | 7%
Eucalyptus essential oil | 23 ℃×24 h | 12%
Prevent leakage of essential oils and active ingredients; resistant to alcohols, glycerin, and other solvents.
Bottle Cap Seals and Gaskets
Resistant to components in lipstick such as tree wax, mineral oil, and vegetable oil.
口红口红塑型软管
Lipstick molding tubes

## Slide 31
Bionic skin：
Offers superior tactile sensing and biocompatibility while protecting internal precision components.
Special sealing：
High oil and heat resistance, suitable for demanding and complex working conditions.
Conductive fluorosilicone rubber：
Integrates EMI shielding and tactile sensing in a single, smart design.
Broadening Application Areas
—— New-Generation Bionic Robots

## Slide 32
Outstanding Performance in New Energy Applications：
With high temperature and corrosion resistance, it serves as an ideal material for sealing and insulation in new energy batteries, significantly enhancing the safety and lifespan of battery packs.
Reliable Protection for Photovoltaic Modules:
Provides encapsulation and frame sealing, effectively resisting UV exposure and extreme weather conditions to ensure long-term stable operation of the modules.
Safety Assurance for Energy Storage Systems:
Offers excellent electrical insulation and chemical resistance, delivering efficient and reliable protection for energy storage systems.
Broadening Application Areas
——New Energy

## Slide 33: Performance Comparison Between Fluorosilicone Rubber and Other Rubbers
Material | Advantage | Limitation
Fluorosilicone Rubber (FVMQ) | Excellent oil resistance across a wide temperature range; well‑balanced overall properties | Higher cost; lower tensile strength compared to fluororubber
Fluorocarbon Rubber (FKM) | Excellent oil resistance and high strength | Poor low-temperature performance (prone to embrittlement above –30 °C)
Silicone Rubber (VMQ) | High-temperature resistance (up to 300 ℃), good flexibility | Poor oil resistance, susceptible to swelling in oils
Acrylate Rubber（ACM） | Excellent oil resistance | Inferior low‑temperature performance

## Slide 34
NEWERA
Thank you.
We welcome your inquiries!